## Slide 1
Glass-Based
Sub-Wavelength Photonic Structures
Andrea Chiappini1, Alessandro Chiasera1, Anna Lukowiak1,2, Davor Ristic1,3, Iustyna Vasilchenko1,4, Brigitte Boulard5, Claire Duverger Arfuso5, Cristina Armellini1,6, Alessandro Carpentiero1,
Stefano Varas1, Simone Normani1,4, Inas K. Battisha7, Gilles Cibiel8, Giancarlo C. Righini9,10,
Maurizio Ferrari1
1IFN – CNR CSMFO Lab., Via alla Cascata 56/C Povo, 38123 Trento, Italy
2Institute of Low Temperature and Structure Research, PAS, 50-422 Wroclaw, Poland
3Ruđer Bošković Institute, P.O. Box 180, 10002 Zagreb, Croatia
4Dipartimento di Fisica, Università di Trento, via Sommarive 14, Povo, 38123 Trento, Italy
5IMMM, UMR 6283, Equipe Fluorures, Université du Maine, Le Mans, France
6FBK Center for Materials & Microsystems, Via Sommarive 18, Povo 38123 Trento, Italy
7National Research Center, 12622 Dokki, Giza, Egypt
8Centre National d’Etudes Spatiales (CNES), 31401 Toulouse Cedex 9, France
9IFAC - CNR, MiPLa.b, Via Madonna del Piano 10, 50019 Sesto Fiorentino, Italy
10Museo Storico della Fisica e Centro di Studi e Ricerche Enrico Fermi, P.zza Viminale 1, 00184 Roma, Italy
CNR DSFTM
Notes: 1

## Slide 2
Institute for Photonics and Nanotechnologies (IFN)
lighting the way ahead
Notes: 2

## Slide 3
                OUTLINE
                Motivation of Glass Photonics Research
                Glass Ceramics
                § Down conversion systems
                § SnO2 nanocrystals as sensitizers
                Photonic Crystals
                § Opals
                § 1D microcavities
                Spherical microresonators
                Conclusions and Perspectives

## Slide 4
Motivation of Glass Photonics Research
CNR DSFTM
Notes: 4

## Slide 5
MOTIVATION
Light control
Nano scale confined structures
Micro scale confined structures
Glass-ceramic waveguides
Photonic crystals (n-D, Fibers)
Colloidal systems
Fibers and Waveguides
Resonators
Cavities
Novel materials, functionalizations, and geometries

## Slide 6: WE START FROM:
AND……………

## Slide 7
Low loss window
(< 0.3 dB/Km) is
200 nm wide
More channels
Largely-spaced
channels
Non-zero dispersion
WDM CHANNELS
25 THz
Range of high Gain EDFAs 4 THz

## Slide 8
          Tb3+ and Yb3+ ions in sol-gel derived
          SiO2-HfO2 glass ceramic planar waveguides
Glass Ceramics and Energy Transfer

## Slide 9: Down conversion with Tb3+/ Yb3+
One green photon @ 488nm
Two red photon @ 980 nm

## Slide 10
10
Low phonon energy ( 700 cm-1)
Rare earth solubility
Combine spectroscopic properties of the crystal with optical properties of the glass
Determine the efficiency of the process
Optimize the rare earth ions content
Down-converters Silica-Hafnia glass ceramics

## Slide 11
Sample label | Terbium concentration in mol% | Ytterbium concentration in mol% | n@543.5 nm TE polarization [± 0.001] | n@632.8 nm TE polarization [± 0.001] | Layer thickness [±0.2µm]
AR1 | 0.5 | 0 | 1.621 | 1.616 | 1.0
A1 | 0.5 | 1 | 1.626 | 1.621 | 1.0
A2 | 0.5 | 2 | 1.631 | 1.626 | 1.0
A3 | 0.5 | 3 | 1.633 | 1.628 | 1.1
BR1 | 0.2 | 0 | 1.623 | 1.617 | 1.1
B1 | 0.2 | 0.8 | 1.604 | 1.608 | 0.9
BR3 | 0.6 | 0 | 1.624 | 1.620 | 1.1
B3 | 0.6 | 2.4 | 1.630 | 1.625 | 1.2
BR5 | 1 | 0 | 1.626 | 1.621 | 1.2
B5 | 1 | 4 | 1.638 | 1.633 | 1.1
Rare earth concentration, refractive index and thickness of the waveguides
Prepared waveguides

## Slide 12
TEM images
Validation of the process: Incorporation of hafnia nanocrystals in the waveguide
Nanocrystals identified as monoclinic HfO2
Size of about 3-4 nm

## Slide 13
Room temperature photoluminescence spectra of the 2F5/22F7/2 transition of Yb3+ ions after excitation at 476 nm for the three samples of the first series. Each spectrum was normalized to the maximum of the luminescence intensity.
The emission of the Yb3+ ion after excitation at 476 nm is a indication of the presence of an efficient energy transfer from Tb3+ to Yb3+.
The TE0 mode waveguiding excitation was used for luminescence measurements, by detecting the light coming out from the waveguide surface. Luminescence spectroscopy was performed using the 476 nm line of an Ar+ ion laser as excitation source at 600 mW power.
However, it is not possible to evaluate the conversion efficiency only on the base of the photoluminescence spectra.
Tb 0.5 mol%
A1 1 mol% Yb
A2 2 mol% Yb
A3 3 mol% Yb
Photoluminescence spectra

## Slide 14
14
Energy transfer efficiency between Tb3+ and Yb3+ :
Decay curves of the luminescence from the 5D4 metastable state of Tb3+ ions for the first samples series under excitation at 355 nm.
The relation between the transfer efficiency and the effective quantum efficiency is linear and is defined as:
ηEQE = ηTb-r(1-ηTb-Yb)+2ηTb-Yb
where the quantum efficiency for Tb3+ ions, ηTb-r, is set equal to 1.
Decay curves analysis

## Slide 15
Transfer efficiency and effective quantum efficiency as a function of Yb3+ molar concentration for A samples where Tb3+ content is fixed at 0.5 mol%
For compositions with Tb3+ content kept constant at 0.5 mol% and increasing Yb3+ molar concentration, we observed that:
the Tb-Yb energy transfer efficiency increases with the increase of the molar ratio Yb/Tb;
the energy transfer efficiency does not exceed 24-25%.
Composition (Yb concentration in mol%) | 1% | 2% | 3%
Estimated transfer efficiency (in glass ceramic) | 14% | 24% | 25%
Estimated effective quantum efficiency (in glass ceramic) | 114% | 124% | 125%
Estimated transfer efficiency (in glass) | 2% | 4% | 6%
Estimated effective quantum efficiency (in glass) | 102% | 104% | 106%
Tb3+/ Yb3+ down conversion efficiency

## Slide 16
Heat Treatment at
900, 1000, 1100 ºC for 30’- 5h
Samples:
92 SiO2 - 8 SnO2 : 1 mol% Eu3+_HT at 800, 900, 1000, 1100C for 30’.
84 SiO2 - 16 SnO2 : 1 mol% Eu3+_HT at 800, 900, 1000, 1100C for 30’.
75 SiO2 - 25 SnO2 : 1 mol% Eu3+_HT at 800, 900, 1000, 1100C for 30’, 1100 C for 1h and 5h.
SnO2-SiO2 Glass-Ceramic Waveguides
S.N.B. Bhaktha, F. Beclin, M. Bouazaoui, B. Capoen, A. Chiasera, M. Ferrari, C. Kinowski, G.C. Righini, O. Robbe, S. Turrell
“Enhanced fluorescence from Eu3+ in low-loss silica glass-ceramic waveguides with high SnO2 content”
Applied Physics Letters 93 (2008) pp. 211904-1/3.
T.T. Van Tran, T. Si Bui, S. Turrell, B. Capoen, P. Roussel, M. Bouazaoui, M. Ferrari, O. Cristini, and C. Kinowski
“Controlled SnO2 nanocrystal growth in SiO2-SnO2 glass-ceramic monoliths”
Journal of Raman Spectroscopy 43 (2012) pp. 869-875.

## Slide 17
TEM
Homogeneous distribution
About 4 nm NCs

## Slide 18
Raman spectra
Crystal-peak observed in the low-frequency region.
Increasing shoulder centered around 550 cm-1 is attributed to the SnO2 crystals.
Boson
Si-O-Si symmetric stretching
T-O-T
(T = Si or Sn)
SnO2 crystal
shoulder
v
Lc
w = Sl,n
w = wavenumber
v = sound velocity
L = particle size
c = speed of light

## Slide 19
Excitation spectra
Room temperature excitation spectra of 5D0 → 7F2 emission at 613 nm
The broad and strong band observed at 310 nm (4.0 eV) corresponds to the SnO2 band-gap energy.
x=mol%SnO2

## Slide 20
PL spectra
5D1
lex=351nm
For annealing temperature higher than 900 °C the emission features typical of Eu3+ ion in a crystalline like environment are predominant, indicating that most part of Eu3+ ions are embedded in SnO2 nanocrystals

## Slide 21: Enhanced fluorescence from Eu3+ in low-loss silica glass-ceramic waveguides with high SnO2 content
S.N.B. Bhaktha, F. Beclin, M. Bouazaoui, B. Capoen, A. Chiasera, M. Ferrari, C. Kinowski, G.C. Righini, O. Robbe, S. Turrell, “Applied Physics Letters 93 (2008) pp. 211904-1/3.
Crack-free and low loss glass ceramic waveguide 75SiO2-25SnO2: Eu3+ fabricated by sol gel, dip-coating method. Losses remain below 0.8 dB/cm.
lex = 351 nm

## Slide 22: High photosensitivity in low-loss sol-gel SiO2 – SnO2 waveguides
Effective index change at 1550 nm for the single mode waveguide after the UV irradiation at 248 nm as a function of cumulative doses used. The solid line is an help for the eyes.
S.Berneschi, S.N.B. Bhaktha, A. Chiappini, A. Chiasera, M. Ferrari, C. Kinowski, S. Turrell, C. Trono, M. Brenci, I. Cacciari, G. Nunzi Conti, S. Pelli, G. C. Righini “Highly photorefractive Eu3+ activated sol-gel SiO2 – SnO2 thin film waveguides”
Proceedings of SPIE Vol. 7604 (2010) pp. 76040Z-1/6

## Slide 23: High photosensitivity in low-loss sol-gel SiO2 – SnO2 waveguides
A swelling of about 4 nm was observed in UV exposed regions
B.N. Shivakiran Bhaktha, Simone Berneschi, Gualtiero Nunzi Conti, Giancarlo C. Righini, Andrea Chiappini, Alessandro Chiasera, Maurizio Ferrari, Sylvia Turrell
“Spatially localized UV-induced crystallization of SnO2 in photorefractive SiO2-SnO2 thin film”.
Proceedings of SPIE Vol. 7719 (2010) pp. 77191B-1/5.
S.Berneschi, S.N.B. Bhaktha, A. Chiappini, A. Chiasera, M. Ferrari, C. Kinowski, S. Turrell, C. Trono, M. Brenci, I. Cacciari, G. Nunzi Conti, S. Pelli, G. C. Righini “Highly photorefractive Eu3+ activated sol-gel SiO2 – SnO2 thin film waveguides”
Proceedings of SPIE Vol. 7604 (2010) pp. 76040Z-1/6

## Slide 24
Opals: a suitable photonic structure for light confinement
CNR DSFTM
Photonic Crystals
Notes: 24

## Slide 25
Silica Spheres
The reaction takes place at room temperature and
we can control the particle size through the concentration of a single reactive.
[TEOS] = 0.22 M
[NH3] = 1.0 M
[H20] = 15.0 M
Molar Concentrations
high uniformity of silica spheres
(less than 5% of dispersion in diameter)
the dimension of :~255nm
Stober Methods
Notes: The starting point to the synthesis the silica submicron spheres is using the so called Stober method. It take place by the hydrolysis and the condesation/polimerisation reactions where the TEOS is using as starting reagents in an alcoholic solution of water and ammonia, where the ammonia itself plays the role of catalyst.
To the take in mind is we can control the particles size through the molar concentration of every single reactives. In our particular case

## Slide 26
3D Photonic Crystals bottom-up approach
Low cost
“Easy”
Self-Assembling
colloidal nano-microspheres
relative easiness of preparation
associated with their manufacture
AFM image of the top surface of the opal formed by spin-coating technique of 236 nm diameter polystyrene spheres.
A.Chiappini, C. Armellini, A. Chiasera, M. Ferrari, L. Fortes, M. Clara Gonçalves, R. Guider, Y. Jestin, R Retoux, G. Nunzi Conti, S. Pelli, Rui M. Almeida, and G.C. Righini. “An alternative method to obtain directs opal photonic crystals structures” Journal of Non-Crystalline Solids 355 (2009) pp. 1167-1170
Notes: Photonic crystals can be viewed just as a subclass of a larger family of
material systems called metamaterials

## Slide 27
Polystyrene monosized spheres
Single-stage polymerization process based on formation and growth of polymeric nuclei dispersed in an emulsion constituted by water, styrene, potassium persulfate (KPS) and sodium docecyl sulfate (SdS).
Control the size of the particles through the concentration
of sodium docecyl sulfate.
Range 150 ÷ ~ 1000 nm
HRTEM characterization of polystyrene spheres synthesized by microemulsion, where an average dimension of 236 nm with a polidispersivity of about 3% is determined
Notes: 27
The main future of the structure of amorphous materials is the absence of the long range order , which it is important to know the structure of the material to understand thear physical and or chemical properties
As we will see after.

## Slide 28
Self Assembly approach
Self Assembly techniques
Vertical Deposition
A. Chiappini, C. Armellini, A. Chiasera, M. Ferrari, Y. Jestin, M. Mattarelli, M. Montagna, E. Moser, G. Nunzi Conti, S. Pelli, G.C. Righini, M. Clara Gonçalves, Rui M. Almeida, "Design of photonic structures by sol–gel-derived silica nanospheres" Journal of Non-Crystalline Solids 353 (2007) pp. 674–678.
Notes: 28
The main future of the structure of amorphous materials is the absence of the long range order , which it is important to know the structure of the material to understand thear physical and or chemical properties
As we will see after.

## Slide 29
Self Assembly techniques
Spin-coating deposition
“Bottom up approch “
C. Armellini, A. Chiappini, A. Chiasera, M. Ferrari, Y. Jestin, E. Moser, G. Nunzi Conti, S. Pelli, A. Quandt, G.C. Righini, C. Tosello
“Er3+ - activated nanocomposite photonic glasses and confined structures”
Optical Materials 31 (2009) pp. 1071-1074.
Notes: 29
The main future of the structure of amorphous materials is the absence of the long range order , which it is important to know the structure of the material to understand thear physical and or chemical properties
As we will see after.

## Slide 30
Silica inverse opals
Latex opals as templates
Polystyrene Colloidal particles
D= 236nm
Monodisperse particles in DW solution.
1
2
3
4
Thermal heat-treatment
HT: 450°C
0.1 °C/min
Silica solution
Spin deposition technique
HT: 900°C
0.3 mol % Er3+

## Slide 31: Inverse structure
Hollow regions of air spheres
well ordered in a triangular lattice corresponding to the (111) planes
of a fcc crystalline strucure.
It’s a negative replica of direct opal (template)
The average dimension of the air-hollows is ~210 nm

## Slide 32
Optical Properties
Bragg’s Law
Filling Factor 23%
Max 26%
Variable incident angle reflectance measurements of inverse opals

## Slide 33
Room temperature photoluminescence spectrum of the 4I13/2 → 4I15/2 transition of Er3+ ions
peak at 1540 nm
1490 nm
1567 nm
1617 nm
16.8±0.1 ms
η= 90%
Luminescence at 1.5µm
C. Armellini, A. Chiappini, A. Chiasera, M. Ferrari, Y. Jestin, E. Moser, R. Retoux, G. Speranza, L. Minati, G. Nunzi Conti, S. Berneschi, I. Cacciari, S. Pelli, G.C. Righini.
“Fabrication and Characterization of Silica Opals”
Advances in Science and Technology Vol. 55 (2008) pp 118-126.

## Slide 34
Photonic Crystals - fundamentals
Why are Photonic Materials special?
Improvement of LED efficiency.
(b) microstructured emitter: light that would not radiate into the emission cone is suppressed by the photonic crystal, i.e. there are no modes for the emission to radiate into, so all spontaneous emission is channeled into the “useful” modes of the device. In principle, the external effiency of such a device can reach the internal efficiency of the material of > 90%.

## Slide 35
Photonic Crystals - application
Superprism effect
The figure shows how the dispersion properties of a photonic crystal can be used. Due to the high dispersion of wavelengths near the band edge, it is possible to separate the spectral contents of an incoming multi-wavelength signal. This particular effect is known as "superprism"

## Slide 36
Photonic Crystals - application
Superprism effect
H. Kosaka, T. Kawashima, A. Tomita, M. Notomi, T. Tamamura, T. Sato, and S. Kawakami “Superprism phenomena in photonic crystals”, Phys. Rev. B 58 (1998) pp. R10 096-R10 099.
The self-organized 3D photonic crystal, with the stacking structure analogous to that of simple hexagonal graphite, employed to demonstrate superprism effect in the optical frequency region.

## Slide 37
Photonic Crystals - application
Superprism effect
Photographs showing light-beam swing inside the photonic crystal. The tilting angle of the incident light was slightly altered from +7° (left) to -7° (right). Both paths show negative bending. The incident light has a wavelength 956 nm (/a=0.33) with TM polarization. The crystal size is 0.5 mm x 0.5 mm.
H. Kosaka, T. Kawashima, A. Tomita, M. Notomi, T. Tamamura, T. Sato, and S. Kawakami “Superprism phenomena in photonic crystals”, Phys. Rev. B 58 (1998) pp. R10 096-R10 099.

## Slide 38
Photonic Crystals - application
Superprism effect
If Snell’s law is applied without regard to the photonic band anisotropy, this phenomenon implies a negative refractive index.
H. Kosaka, T. Kawashima, A. Tomita, M. Notomi, T. Tamamura, T. Sato, and S. Kawakami “Superprism phenomena in photonic crystals”, Phys. Rev. B 58 (1998) pp. R10 096-R10 099.

## Slide 39
Photonic Crystals - application
Superprism effect
H. Kosaka, T. Kawashima, A. Tomita, M. Notomi, T. Tamamura, T. Sato, and S. Kawakami “Superprism phenomenaSuperprism Phenomena in Photonic Crystals: Toward Microscale Lightwave Circuits”, Journal of Lightwave Technology, 17 (1999) pp. 2032-2038.
 10°
Conventional prism
X 500
Superprism
made of Photonic Crystal
~ 50°
Dl = 1%
0.99 mm – 1mm
l3
l2
l4
l1
l1>l6
l5
l6

## Slide 40
Photonic Crystals - application
Superprism effect
H. Kosaka, T. Kawashima, A. Tomita, M. Notomi, T. Tamamura, T. Sato, and S. Kawakami “Superprism phenomenaSuperprism Phenomena in Photonic Crystals: Toward Microscale Lightwave Circuits”, Journal of Lightwave Technology, 17 (1999) pp. 2032-2038.
(a) light paths inside a PC with incident light of 0.99-mm and 1.0-mm wavelengths. A large swing reaching 50° was achieved with a slight wavelength change of 1%. The incident light was polarized in the TM mode and tilted at 15° from normal to the crystal edge and
(b) light propagation in a conventional Si crystal under the same condition as (a). The two beams with different wavelengths traced almost the same paths.

## Slide 41
Photonic Crystals - application
Superprism effect: 1D superprism (plan view)
A. Bakhtazad, A.G. Kirk, “Superprism effect with planar 1-D photonic crystal”, Proceedings of the SPIE, Volume 5360, pp. 364-372 (2004)

## Slide 42
Strain Sensor
Material: Changing the structural color under an external stimulus
Blue shift of the wavelenght of the diffraction peak as a function of the applied strain
Recognize this by naked eyes
How it works?

## Slide 43
Strain Sensor
Experimental validation
D. Zonta, A. Chiappini, A. Chiasera, M. Ferrari, M. Pozzi, L. Battisti, M. Benedetti, Proc. of SPIE 7292 (2009) pp. 729215-1 - 729215-10.
Initial
Applied strain
Experimental set-up
L + ΔL
L

## Slide 44
Strain Sensor
Response Characterisation
D. Zonta, A. Chiappini, A. Chiasera, M. Ferrari, M. Pozzi, L. Battisti, M. Benedetti, Proc. of SPIE 7292 (2009) pp. 729215-1 - 729215-10.
d111, decreases linearly
the position of the peak does not change significantly,
Inter lanar distance remains constant for the applied strain,
since the PS spheres are in contact with each other
Peak position blue shifts from 583 to 550 nm
Linear response

## Slide 45
  Strain sensor
  SERS substrate
Metallo – dielectric structures
Possible applications

## Slide 46
Gold nanoparticles
How to prepare?
Turkevich Method (1951)
Turkevich, J.; Stevenson, P. C.; Hillier, J. Nucleation and Growth Process in the Synthesis of Colloidal Gold. Discuss. Faraday Soc. 1951, 11, 55-75.
Reduction of Gold ion by citrate ions
+
LSPR = 520 nm
chloroauric acid
chloroauric acid
chloroauric acid
Notes: 46
First metallic nanostructures investigated were nano-particles.
see different sized colloids in solution.
Faraday noted that the colour of the particles depend on size.
Particles give fields at surface so used for SERS, but difficult coupling and poor reproducibility.
Voids, colour tunes with size. Easy coupling by geometry.

## Slide 47
Structural Properties
Inverse ordered structure is still present after immersion process
hollow regions of the air spheres
(well ordered in a triangular lattice corresponding
to the (111) planes of a fcc crystalline structure)
inner dark holes
(representing the point of contact between each
templating sphere and its 12 nearest neighbors)
After 2 h immersion time
Au Nps are attached/immobilized on the network of the ISO system
After 10 h immersion time
Notes: 47
The main future of the structure of amorphous materials is the absence of the long range order , which it is important to know the structure of the material to understand thear physical and or chemical properties
As we will see after.

## Slide 48
Raman Signal Enhancement
benzenethiol (BT) as a probe molecule
1x10-3M
MDCS systems have been tested as SERS substrate
to evaluate the efficiency of the MDCS
using a 10 s accumulation time, incidence power 100 µW.
we have compared the Raman signal obtained for these structures with those collected :
b) on a gold film (GF) deposited by sputtering
c) on ISO spotted with a 5 µl drop of pure BT and left to dry out (ISO_BT).
Notes: 48
The main future of the structure of amorphous materials is the absence of the long range order , which it is important to know the structure of the material to understand thear physical and or chemical properties
As we will see after.

## Slide 49
Raman Signal Enhancement
Notes: 49
The main future of the structure of amorphous materials is the absence of the long range order , which it is important to know the structure of the material to understand thear physical and or chemical properties
As we will see after.

## Slide 50
HIGH QUALITY FACTOR 1-D Er3+-ACTIVATED DIELECTRIC MICROCAVITY FABRICATED BY RF-SPUTTERING
CNR DSFTM
Photonic Crystals
Notes: 50

## Slide 51
TiO2 Target
SiO2 Target
SiO2 + Er Target
Substrate: v-SiO2, dim. 7 x 3cm
Deposition is performed by sputtering alternatively the targets of silica and titania. The depositions were tailored to reach the appropriate thicknesses to obtain a cavity resonance centred at 1.7 m
Fabrication Protocol – Target composition
Bragg Mirror 10 alternated quarter wave layers TiO2 and SiO2
TiO2 n = 2.20 (@ 1550 nm)
SiO2 n = 1.44 (@ 1550 nm)
Active layer half wave SiO2 activated with Er3+ ions.
SiO2
TiO2

## Slide 52
1-D microcavities fabricated by RF-sputtering
Development and optical and spectroscopic diagnostic of photonic materials and structures
Bragg Mirror: 20 alternated quarter wave layers TiO2 (170 nm) and SiO2 (320 nm).
Active layer: half wave (640 nm) SiO2 activated with 0.2 mol % of Er3+.
The dark regions corresponds to SiO2 and the white regions corresponds to TiO2
S. Valligatla, A. Chiasera, S. Varas, N. Bazzanella, D.N. Rao, G.C. Righini, M. Ferrari, “High quality factor 1-D Er3+-activated dielectric microcavity fabricated by RF-sputtering”, Optics Express, Vol. 20 Issue 19, pp.21214-21222 (2012)

## Slide 53
Transmittance spectrum of the cavity with two Bragg reflectors. The stop band range from 1490 to 1980 nm. The cavity resonance corresponds to the sharp maximum centred at 1.749 µm. The FWHM of the resonance is 1.97 nm that correspond to a quality Q factor of 890.
Transmission measurements

## Slide 54
Schematics of the excitation and detection geometries employed for a reliable assessment of the influence of the cavity on the 1.5 mm emission band of Er3+ ion.
Fig. (a): configuration employed for the Er3+-activated reference sample:
Fig. (b): configuration employed for the Er3+-activated 1-D microcavity.
4I13/2→4I15/2 photoluminescence spectra of the cavity activated by Er3+ ion in 1-D photonic crystal and of the single Er3+-doped SiO2 active layer with first Bragg mirror. The light is recorded at 50° from the normal on the samples upon excitation at 514.5 nm.

## Slide 55
Whispering Gallery Modes
Laser
CNR DSFTM
Spherical microresonators
Notes: 55

## Slide 56: Spherical microresonators WGMs
Microsphere of diameter d and refractive index ns coated by a film of thickness t and refractive index nc.
G.C. Righini, Y. Dumeige, P. Féron, M. Ferrari, G. Nunzi Conti, D. Ristic, S. Soria., “Whispering gallery mode microresonators: fundamentals and applications”, Rivista del Nuovo Cimento 34 (2011) pp. 435-488.
D. Ristić, A. Rasoloniaina, A, Chiappini, P. Féron, S. Pelli, G. Nunzi Conti, M. Ivanda, G.C. Righini, G. Cibiel, and M. Ferrari “About the role of phase matching between a coated microsphere and a tapered fiber: experimental study” Optics Express, 21 (2013) pp 20954-20963

## Slide 57
 | F1 | F2 | F3 | F4 | F5 | F6 | F7 | F8 | F9
d/μm [±5 μm] | 155 | 135 | 140 | 140 | 140 | 145 | 130 | 155 | 145
Ellipticity [±1%] | 4% | 7% | 4% | 5% | 7% | 5% | 4% | 3% | 3%
Microscope images of the F5 microsphere before and after coating
Before coating
After coating
Silica microspheres fabricated by melting a SMF-28 rod. This glass presents a very low concentration of impurities (<0.3 ppm) and OH groups (<0.2 ppm), the attenuation coefficient is very low ( 0.2 dB/km at 1550 nm) The diameters and ellipticity are also reported
Glass coated microspheres

## Slide 58
A waveguide was prepared as reference using the same sol and the same dip coating technique as for the microsphere in order to estimate the thickness and the refractive index of the coating
Glass coated microspheres
Thickness, refractive index, and modal parameters of the planar waveguide used as reference for the sol gel coating of the microsphere. Values are obtained by m-line measurement. The film composition was 70SiO2-30HfO2 activated with 0.3 mol% Er3+.

## Slide 59
Glass coated microspheres
Room temperature photoluminescence spectra and decay curves of the 4I13/2  4I15/2 transition of Er3+ ions for the sol gel coated spherical microresonators and the planar waveguide used as reference. The film composition was 70SiO2-30HfO2 activated with 0.3 mo% Er3+.
All the photoluminescence spectra showed that the deposited films are amorphous, and that there is no difference between the shape of the spectra of different microspheres and the waveguide, indicating that the coating procedure is reproducible.

## Slide 60
Two quantities were measured:
-The surface roughness
-The number of defects/μm2
Glass coated microspheres – AFM

## Slide 61
Defect types
small defects (around 5 nm in height)
Big defects (>15 nm in height)
Holes (10 nm in depth)
A low number of defects is needed to achieve high Q-factors
Glass coated microspheres – Defects

## Slide 62
Uncoated
Coated
For the surface roughness measurements the areas with no defects were chosen
Glass coated microspheres – Roughness

## Slide 63
A 4th order bidimensional subtraction plus an histogram line-by-line levelling has been applied before computing the roughness
Roughness calculated on 2x2 µm2 areas
Defects counted on a
    20x20µm2 image
    10x7µm2 image
Defect density definition: (objects with Zmax>2 nm) numb./µm2
Glass coated microspheres – Surface assessment

## Slide 64
Glass coated microspheres – Near Field
The effective refractive index of the 70SiO2-30HfO2 coated microsphere as a function of the radius of the silica sphere for the fundamental equatorial (n=0; l-|m|=0) TE mode at 1560 nm. The refractive index of the sphere is 1.44 and of the coating 1.6. The coating thicknesses, given in μm, are also reported in the figure. The blue lines correspond to the border cases of no coating (blank sphere) or of very thick coating (bulk sphere with n=1.6). The horizontal dashed line corresponds to the effective refractive index of the propagation mode of a silica fiber taper with a waist of 3 μm. The vertical dashed line correspond to a silica sphere diameter of 155 μm which is the diameter of the sphere coated in our experiment.
Optics Express, 21 (2013) pp 20954-20963 “About the role of phase matching between a coated microsphere and a tapered fiber: experimental study “
Effect of the coating thickness on the coupling efficiency

## Slide 65
d [μm] | l | R [μm] | E (sphere) | E (coating) | E (air)
0.2 | 388 | 68.0056 | 0.88637 | 0.05826 | 0.05537
0.3 | 391 | 68.0616 | 0.79013 | 0.13292 | 0.07695
0.5 | 400 | 67.9925 | 0.55117 | 0.3473 | 0.10153
0.7 | 409 | 67.996 | 0.38182 | 0.52335 | 0.09483
1 | 418 | 67.9822 | 0.23697 | 0.68933 | 0.07371
1.3 | 423 | 67.9418 | 0.15764 | 0.78497 | 0.05738
R= 68 μm
d= 0.5 μm
l = 400
N = 0
We need:
high amount of E. field in the coating
a reasonably long evanescent tail
Glass coated microspheres – Near Field
Effect of the coating thickness on the coupling efficiency

## Slide 66
Glass coated microspheres – Laser WGMs
The average integrated luminescence in the 1535-1585 nm range for the 0.3 mol% Er3+ 70SiO2-30HfO2 coated sphere in respect to the number of dips and to the percentage of the fundamental WGM electric field (e. f.) inside the coating as calculated from the number of dips.
Effect of the coating thickness on the coupling efficiency

## Slide 67
Glass coated microspheres – Near Field
The effect of the coating on the whispering gallery modes was studied
The coating used was 70 % SiO2 – 30% HfO2 doped with 0.3 mol % Er3+
The spheres (D=140±10 μm) were characterized using a tapered fiber

## Slide 68
Excitation at 1.48 μm
Laser power:  120 mW.
The peak power of the detected modes was always in the range of nanowatts, the highest power detected being 30 nW.
WGM modes are clearly visible
Different modes are excited depending on the position of the taper
N=1.6
λ = 1550 nm (wavelength of the signal)
FSR is 3.7 nm corresponding to a microsphere of about 130 μm
Q-factor is greater than the resolution of our detector (>3x104)
Glass coated microspheres – Laser WGMs

## Slide 69
Thermal effects of coatings
Alessandro Chiasera, Yannik Dumeige, Patrice Féron, Maurizio Ferrari, Yoann Jestin, Gualtiero Nunzi Conti, Stefano Pelli, Silvia Soria, and Giancarlo C. Righini.“Spherical whispering-gallery-mode microresonators”Laser & Photonics Reviews 4 (2010) pp. 457-482
Another important application of transparent coatings onto spherical microresonators concerns the possibility of reducing the thermal shift of the WGM resonances due to microsphere heating by the dissipated pump energy.
Actually, the shift is due both to the temperature-induced change in the refractive index (the thermo-optic coefficient) and to the temperature-induced increase of the diameter of the sphere (coefficient of thermal expansion)

## Slide 70
Thermal effects of coatings
Alessandro Chiasera, Yannik Dumeige, Patrice Féron, Maurizio Ferrari, Yoann Jestin, Gualtiero Nunzi Conti, Stefano Pelli, Silvia Soria, and Giancarlo C. Righini.“Spherical whispering-gallery-mode microresonators”Laser & Photonics Reviews 4 (2010) pp. 457-482
λ is the WGM wavelength
T is the temperature
α is the thermal-expansion coefficient
N is the refractive index of the microsphere
One can also take advantage of this characteristic of the spherical WGMRs to accurately measure the thermo-optic coefficient of the material of which the microresonator is made

## Slide 71
Thermal effects of coatings
No red shift increasing pump power
due to the silica-hafnia coating
Whispering gallery modes emission spectra of a silica microsphere of 250 m in diameter and coated by a film of 70SiO2-30HfO2 activated with 1 mol% Er3+. The thickness of the coating is 0.8 m. Spectra are obtained at different current of the 1480 nm pump laser.
Alessandro Chiasera, Yannik Dumeige, Patrice Féron, Maurizio Ferrari, Yoann Jestin, Gualtiero Nunzi Conti, Stefano Pelli, Silvia Soria, and Giancarlo C. Righini.“Spherical whispering-gallery-mode microresonators”Laser & Photonics Reviews 4 (2010) pp. 457-482

## Slide 72
Photonic crystals that exhibit specific morphologic, structural, and optical properties allow to develop interesting new physical concepts, as well as novel photonic devices based on the control of the light.
RF – sputtering and colloidal route are complementary techniques suitable for fabrication of high Q 1-D photonic microcavities and versatile 3-D photonic opals activated by rare earth ions, respectively.
WGMs laser or frequency combs can be tailored by suitable coating of spherical microresonators
Conclusions and Perspectives
ACKNOWLEDGEMENTS:
CNES SHYRO project (2011-2015)
NSBMO research project (2010-2013)
Polish Ministry of Science and Higher Education “Mobility Plus” Program
SiMeCro research project (2012-2013) Caritro Foundation
MAE Significant Bilateral Project between Italy and Egypt titled “Smart optical nanostructures for green photonics (2013-2015)

## Slide 73
Welcome to
CIMTEC 2014
Montecatini Terme, Italy - June 9-20, 2014 13th International Ceramics Congress (June 9-13, 2014)
& 6th Forum on New Materials (June 16-20, 2014)
Symposium CL Inorganic Materials Systems for Optical and Photonic Applications
XVIth International Krutyn Summer School 2014, Krutyń, Masurian Lake District, Poland, August 31-September 6, 2014
http://glassphotonics.ikss.eu/
Lanthanide-based photonic materials and structures: breakthrough applications and cutting edge systems